Section Cover Page

Section 02841 2000-03-22 Road and Parking Appurtenances

Use this Section to specify supply and installation of products listed.  Specify supply and installation of premanufactured car plug-in posts in Division 16.  Specify electrical requirements in Division 16.

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Sections

1.2	Product Options and Substitutions

1.3	Detail Drawings

1.4	Coordination

2.	Products

2.1	Concrete Bases

2.2	Metal Car Plug-In Rails and Posts

2.3	Wooden Car Plug-In Rails

2.4	Guard Posts

2.5	Premanufactured Curbs

2.6	Site Painting and Finishing Materials

2.7	Fabrication of Metal Components

3.	Execution

3.1	Installation, General

3.2	Installation of Concrete Bases

3.3	Installation of Wooden Car Plug-In Rails

3.4	Painting and Finishing

3.5	Site Painting and Finishing Schedule

.3	Detail Drawings:

02841.01	Street Light Base

02841.02	Metal Car Plug-In Rail

02841.03	Metal Car Plug-In Rail (Hollow Structural Steel Beam)

02841.04	Wooden Car Plug-In Rail

02841.05	Metal Pedestal Plug-In Post

02841.06	Guard Post Detail

02841.07	Precast Concrete Curb

Applicable Standards:

.1	CSA A23.4-94	Precast Concrete - Materials and Construction

.2	CSA G30.18-M92	Billet Steel Bars for Concrete Reinforcement

.3	CAN/CSA-G40.20-M92	General Requirements for Rolled or Welded Quality Steel

.4	CAN/CSA-G40.21-M92	Structural Quality Steels

.5	CAN/CSA G164-M92	Hot Dip Galvanizing of Irregularly Shaped Articles

.6	CAN/CSA-O141-91	Softwood Lumber

These reference documents may be available for reference purposes in the Technical Resources and Standards Branch Library, Alberta Infrastructure, 3rd Floor, 6950 - 113 Street, Edmonton; Telephone:  (780) 427-7924.

1.	General

1.1	RELATED SECTIONS

.1	Site Excavating, Filling and Grading: 	Section 02320.

.2	[Custom Steel Fabrications:	Section 05501].

.3	[Site Painting and Finishing General Requirements:	Section 09901].

.4	[Exterior Site Painting and Finishing Schedules:	Section 09902].

.5	Electrical components and installation:	Division 16.

.6	[Premanufactured Car Heater Posts:	Section [    ].

.7	[Poles and Standards:	Section 16529].

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 1 for requirements pertaining to product options and substitutions.

1.3	DETAIL DRAWINGS

.1	The following detail drawings are appended hereto and form part of this Section:

Number	Title

02841.01	Street Light Base

02841.02	Metal Car Plug-In Rail

02841.03	Metal Car Plug-In Rail 1	(Hollow Structural Steel Beam1

02841.04	Wooden Car Plug-In Rail

02841.05	Metal Pedestal Plug-In Post

02841.06	Guard Post Detail

02841.07	Precast Concrete Curbs

SPEC NOTE:  Include only those Detail Drawings applicable to the Project.  Coordinate project working drawings with Detail Drawings.  Delete detail for precast concrete curbs if only plastic curbs are specified.

SPEC NOTE:  If soils report indicates unusual conditions, design of concrete bases may have to be revised from standard detail drawings.

1.4	COORDINATION

.1	Coordinate anchor bolt locations for street lights with Section 16529.

.2	Coordinate anchor bolt locations for premanufactured plug-in posts with Section [    ].

.3	Coordinate requirements for electrical components to be embedded in concrete or concealed in steel components with work specified in Division 16.

2.	Products

2.1	CONCRETE BASES

.1	Reinforcing Steel:  deformed steel bars to CSA G30.18-M92.

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal] [Type 50-sulphate resistant].

.3	Anchor Bolts and Nuts:  steel, hot dip galvanized to CAN/CSA G164-M92, as detailed.

2.2	METAL CAR PLUG-IN RAILS AND POSTS

SPEC NOTE:  Specify premanufactured plug-in posts in Division 16.

.1	[Steel Sections and Plates:  to CAN/CSA-G40.20-M92 and CAN/CSA-G40.21-M92, Grade [260W][   ]].

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal][Type 50-sulphate resistant].

.3	Reinforcing Steel:  deformed steel bars to CSA G30.18-M92, as detailed.

.4	Shop Primer:  shop standard compatible with site painting and finishing materials.

2.3	WOODEN CAR PLUG-IN RAILS

.1	Wood:  douglas fir, pine or hemlock, kiln-dried, S4S dimension lumber to CAN/CSA-O141-91, preservative pressure-treated.

.2	Nails, Spikes & Straps:  steel, hot-dip galvanized.

2.4	GUARD POSTS

SPEC NOTE:  Detail drawing 02841.6 at end of this Section describes guard posts for protection to site elements not generally exposed to vehicle traffic, e.g. electrical transformers.  Amend drawing as required where greater exposure to vehicle traffic is anticipated, e.g. at vehicle entrance doors.

.1	Steel Post:  to CAN/CSA-G40.20-M92 and CAN/CSA-G40.21-M92, Grade [260W][   ].

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal] [Type 50-sulphate resistant].

.3	Shop Primer:  shop standard compatible with site painting and finishing materials.

2.5	PREMANUFACTURED CURBS

SPEC NOTE:  Specify either concrete or plastic curbs, or, if both are acceptable, specify both at Contractor's option.  Edit article accordingly.  Plastic curbs may be subject to lateral deflection.

[.1	Provide concrete or plastic curbs, at Contractor's option.]

.[2]	Concrete Curbs:  as indicated on detail drawing and as follows:

.1	Concrete: to CSA A23.4-94, smooth finish.

.2	Reinforcing Steel:  deformed steel bars to CSA G30.18-M92.

.3	Anchor Pins:  as detailed on drawing.

.[3]	Plastic Curbs:  recycled plastic, grey, as manufactured by Futureplast or Elsro, and as follows:

.1	Minimum Dimensions: 114 mm high x 150 mm wide x 1800 mm long.

.2	Anchor Pins:  deformed reinforcing steel to CSA G30.18-M92, diameter for friction fit, minimum 900 mm long.

2.6	SITE PAINTING AND FINISHING MATERIALS

SPEC NOTE:  This Section assumes site painting and finishing materials applies to new work only.  For exterior site repainting and refinishing requirements refer to Section 09903.

.1	As specified in Sections 09901 and 09902.

OR

SPEC NOTE:  Delete previous paragraph and specify following paragraph if roadway and parking appurtenances is part of a separate site development contract and Sections 09901 and 09902 are not used.

.1	Use products listed in Chapter 5, Products List, of the Canadian Painting Contractors Association (CPCA) Manual, and as specified in Site Painting and Finishing Schedule.

2.7	FABRICATION OF METAL COMPONENTS

.1	As specified in Section 05501.

OR

SPEC NOTE:  Delete previous clause and specify the following if roadway and parking appurtenances is part of a separate site development contract and Section 05501 is not used.

.1	Fabricate components square, straight, true, free from warpage and other defects.  Accurately cut, machine, file and fit joints, corners, copes and mitres.

.2	Remove loose mill scale, rust, oil, grease, dirt and other foreign matter using one or more of the following methods:

.1	solvent cleaning

.2	wire brushing

.3	power wire brushing

.4	sandblasting

.3	Apply primer to bare steel within six hours after blast cleaning, in accordance with manufacturer's recommendations.

.4	Apply thick layer of asphaltic paint to concealed surface of base plates to be set into concrete.  Allow to dry before installation.

3.	Execution

3.1	INSTALLATION, GENERAL

.1	Install components square, straight and true to line.  Securely anchor components and accessories in place.

3.2	INSTALLATION OF CONCRETE BASES

.1	Do not pour concrete against frozen surfaces.

.2	Correctly relocate items displaced during concrete placement.

3.3	INSTALLATION OF WOODEN CAR PLUG-IN RAILS

.1	Compact bottom of wood post holes to provide firm foundation.  Backfill in 150 mm layers.  Compact each layer before placing succeeding layer.

.2	Leave a depression 150 mm deep around wood posts until painting is completed, then fill to finished grade level.

3.4	PAINTING AND FINISHING

.1	As specified in Sections 09901 and 09902.

OR

SPEC NOTE:  Delete previous paragraph and specify following paragraph if roadway and parking appurtenances is part of a separate site development contract and Sections 09901 and 09902 are not used.

.1	Comply with Canadian Painting Contractors' Architectural Specification (CPCA) Manual.

.2	Treat cut tops of wood posts and cut ends of wood rails with two coats of wood preservative prior to application of primer.

3.5	SITE PAINTING AND FINISHING SCHEDULE

SPEC NOTE:  Delete this article if Section 09902 is used.  Edit to suit project requirements.

| Substrate | Finish System | Product No. |
| --- | --- | --- |
| Wood | EXT 1-A Alkyd Finish |  |
|  | 1st Coat: Alkyd or Oil Primer | 5 or 7 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 1-B Latex Finish |  |
|  | 1st Coat: Alkyd or Oil Primer | 5 or 7 |
|  | 2nd Coat: Latex | 10, 11, 119 |
|  | 3rd Coat: Latex | 10, 11, 119 |
|  | EXT 1-C Semi-Transparent Stain Finish |  |
|  | 1st Coat: Semi-Transparent Oil Stain | 13 |
|  | 2nd Coat: Semi-Transparent Oil Stain | 13 |
|  | EXT 1-D Solid Colour Stain Finish |  |
|  | 1st Coat: Solid Colour Oil Stain | 14 |
|  | 2nd Coat: Solid Colour Oil Stain | 14 |
|  | EXT 1-E Latex Solid Colour Stain Finish |  |
|  | 1st Coat: Solid Colour Oil Stain | 16 |
|  | 2nd Coat: Solid Colour Oil Stain | 16 |
| Steel | EXT 11-A Alkyd Finish |  |
|  | 1st Coat: Alkyd Metal Primer | 23,24 or 25 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 11-B Quick Dry Spray Finish |  |
|  | 1st Coat: Quick Dry Primer | 95 |
|  | 2nd Coat: Quick Dry Enamel | 96 |
|  | 3rd Coat: Quick Dry Enamel | 96 |

3.5	SITE PAINTING AND FINISHING SCHEDULE (CONTINUED)

| Substrate | Finish System | Product No. |
| --- | --- | --- |
| Steel (cont'd) | EXT 11-C Aluminum Paint Finish |  |
|  | 1st Coat: Alkyd Metal Primer | 23,24 or 25 |
|  | 2nd Coat: Aluminum Paint | 1 |
|  | 3rd Coat: Aluminum Paint | 1 |
|  | EXT 11-D Two Component Epoxy Finish |  |
|  | 1st Coat: Primer | 101 Type I |
|  | 2nd Coat: Two Component Epoxy | 98 or 77 |
|  | 3rd Coat: Two Component Epoxy | 98 or 77 |
|  | EXT 11-E Water Based Epoxy Finish |  |
|  | 1st Coat: Rust Inhibitive Primer | 128 |
|  | 2nd Coat: Water Based Coating | 115 |
|  | 3rd Coat: Water Based Coating | 115 |
| Galvanized | EXT 12-A Alkyd Finish |  |
| Metal |  |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 12-B Aluminum Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Aluminum Paint | 1 |
|  | 3rd Coat: Aluminum Paint | 1 |
|  | EXT 12-D Latex Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Acrylic Latex | 10, 11, 119 |
|  | 3rd Coat: Acrylic Latex | 10, 11, 119 |
|  | EXT 12-E Latex Dry Fall Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Latex Dry Fall | 118 |

END OF SECTION